Made in Denmark!

Importer: Ltd “Abschliff Latvija”

Riga, A Čaka iela 107 K2

Phone: +371 67843844, 67843845

Mob.: +371 26177888

E-mail: info@abschliff.lv

www.abschliff.lv

#### Open: Monday to Friday – 9ºº-18ºº, Saturday- 10ºº-14ºº, Sunday  –  closed

WOCA Master Colour Oil – oiling of wooden floors

Description: Master Colour Oil offers both color and protection in a single product. It deeply penetrates the wood, creating a durable surface with excellent resistance to water and dirt. Ideal for indoor use on all unfinished, new, or newly sanded wood surfaces across all wood species. Advantages:

- Resistant to dirt and fluids, e.g. water, coffee, tea and red wine;

- Available in many different colours;

- Gives the wood a beautiful, breathable surface;

- Indoor climate labelled.

Application area: For untreated, new or newly-sanded wooden surfaces.

Treatment:

- Product, room and floor temperature must be between 15-30°C. Wood humidity must not exceed 12%. Ensure good ventilation during

application and when drying.

- The wood must be newly sanded, use grit 100-120 for the final sanding. Vacuum thoroughly.

- Clean the wood with WOCA Intensive Wood Cleaner and leave it to dry for at least 8 hours before applying the oil.

- Always remember to test on a less visible spot to check the compatibility of the surface with the product.

- Thoroughly shake the container of Master Colour Oil, both before and during use. Containers with different batch numbers should be mixed               	to avoid colour mismatch.

- Apply the oil using a short-bristled paint roller (4-6 mm) in an even coat. Work in small areas  of no more than 10 m² at a time.

- Leave the oil to soak in for 10-20 min. If the oil soaks quickly into the wood, apply more oil.

- Polish the oil into the wood until the surface appears saturated. Use a buffing machine with a beige pad for large areas and a polishing	cloth/pad manually for small areas. Remove excess oil with dry, lintfree cotton cloths or pads until the surface no longer appears wet.

- Continue until the whole area has been polished and excess oil has been thoroughly removed.

- To ensure a good saturation the surface should be re-polished with 1 dl Master Colour Oil per 10 m2 within 6-12 hours after the first 	application. The oil should be polished thoroughly, as described earlier.

Please note: Do not expose the surface to water or clean it for the first 7 days while the oil is hardening. After 7 days the floor can be cleaned with WOCA Natural Soap, which gives the surface extra protection.

Drying time: 12-24 hours at 20°C.

Fully hard: 7 days at 20°C.

Technical data: VOC: 140 g/l, maximum VOC content (A/i (SB)): 500 g/l. Density: 0.90-0.95 g/ml. Shelf life: 3 years. Application Temperature: +15-25°C and approx. 50% air humidity. Coverage: 10-12 m²/l. Colours: Natural, White, Brazil Brown, Castle Grey, Extra White, Walnut, Black, Extra

Grey. Cleaning of tools: Use WOCA Solvent or turpentine. Storage: +10-25°C. Keep out of reach of children. Do not expose to heat (e.g. sunlight).

Store frost-free during winter and cool during summer. Packaging: 750 ml, 1 l, 2.5 l, 5 l. Dilution: WOCA Solvent (does not normally need to be diluted). Solid content: 50-55%.

Maintaining and cleaning: For daily cleaning, WOCA Natural Soap is recommended, which effectively washes and cares for the wood. Supplement occasionally with WOCA Oil Refreshing Soap, which also adds a little oil to the wood with each wash. Maintain with Maintenance Oil or Maintenance Gel as needed..